Yingde Guocai Fine Chemical Limited Company

Tel：86-763-2811205	Fax：86-763-2811024

Address：Kaidi Industrial Park, genggukeng, Taiping Village, Baisha Town, Yingde City, Guangdong Province

Aliphatic Polyurethane Adhesive Resin PU-1001

Product Description

PU-1001 is an aliphatic anionic waterborne polyurethane dispersion with strong adhesion, used to improve interlayer adhesion.

Supply Form

Approx. 22% solids aqueous dispersion.

Technical Data

| Item | Index | Unit | Test method |
| --- | --- | --- | --- |
| Appearance | Translucent liquid with blue light |  | Visual |
| Solid content | 22±1 | % | 150°C, 30 min, forced-air oven |
| Viscosity (25°C) | <500 | mPa·s | GB/T 2794-2022 |
| pH value (diluted 1:10 in water) | 7.0-9.0 |  | GB 6920-86 |
| Density (25°C) | Approx. 1.06 | g/cm³ | GB/T 4472-2011 |

Product Features

- Very soft film formation;

- Excellent adhesion;

Application

PU-1001 forms a very soft film with strong adhesion, suitable for use alone as a tie coat or blended with other materials to improve interlayer adhesion and physical properties without increasing coating stiffness.

Storage

Store in a ventilated, dry area at 5-35°C; protect from freezing. Shelf life is 6 months from shipment. Products older than 6 months should be re-evaluated before use.